Inspection Checklist / 检验单

6061-T6 Seamless Aluminum Tube · DOHO CO., LTD. ↔ Shandong Botong Aluminum Technology · Rev.0 (2026-08-11)

| PO / Lot No. |  | Size 规格 |  | Date 检验日期 |  |
| --- | --- | --- | --- | --- | --- |
| Inspector 检验员 |  | Place 地点 |  | Qty 数量 |  |

Scope: pre-shipment inspection at Botong (report + photos to be shared) and incoming inspection at DOHO, using the same items below. Please record per piece. Values marked ★ are our proposal — to be mutually confirmed in writing before the PO. 适用范围: 装运前由博通按本表检验(提供报告和照片)，到货后DOHO按同一项目复检。请逐支记录。带★数值为我方建议值，下单前双方书面确认。

# A. Dimensions 尺寸

| # | Inspection item 检验项目 | Criteria 标准 | Method & points 方法·位置 | Record 记录 | P/F 判定 |
| --- | --- | --- | --- | --- | --- |
| A1 | Outer diameter 外径 | Nominal +0.05 / −0.00 mm (all measuring points) 公称 +0.05/−0.00 mm | Both ends (50 mm in) + middle, 2 directions (0°/90°) each = 6 readings 两端(距端口50mm)+中间, 每处0°/90° 共6点 |  |  |
| A2 | Wall thickness uniformity ★KEY 壁厚均匀度 ★重点 | Within one section: max−min ≤ 0.1×t ★ / along length (ends vs middle): mean difference ≤ 0.1×t ★ / lower limit: nominal −0 mm 同一断面内 max−min ≤ 0.1×t ★ / 全长平均差 ≤ 0.1×t ★ / 下限: 公称 −0mm | Ultrasonic gauge — 3 sections (both ends + middle) × 4 circumferential points (0°/90°/180°/270°) = 12 readings per piece 超声波测厚仪, 每支12点 |  |  |
| A3 | Roundness 圆度 | Deviation over 360° ≤ 0.5 mm (every section) 360°偏差 ≤ 0.5 mm | 3 sections (both ends + middle), dial gauge full rotation or pi tape 两端+中间, 千分表旋转测量 |  |  |
| A4 | Cut-end roundness (cutting distortion) 切口圆度 | Same criteria as A3 within 50 mm of each cut end — no ovality or flattening from cutting 切口50mm内与A3同一标准, 不得因切割产生椭圆·压扁 | Measure separately at 50 mm from each cut end right after cutting; record apart from A3 切割后在距切口50mm处单独测量记录 |  |  |
| A4b | One-piece over full length ★ 整体一次成型 ★ | Each tube must be one continuous extruded piece over the full length (3 m / 2 m) — joined or welded construction is not acceptable for this product 每支管须全长整体一次成型, 本产品不接受焊接拼接 | All pieces: full-length visual check + full-length UT scan; X-ray photos on lot samples (scope ★ to be agreed — see note below) 全数: 目视+全长超声波扫查, 每批抽样X光拍照(范围★双方商定) |  |  |
| A5 | Length 长度 | 3,000 +10 / −0 mm ★ (Group A·B: 2,000 +10/−0 ★) 3,000 +10/−0 mm ★ | Steel tape, once per piece 钢卷尺 |  |  |
| A6 | Straightness (bow) 直线度 | ≤ 1 mm/m, ≤ 3 mm over full length ★ ≤ 1 mm/m, 全长 ≤ 3 mm ★ | Surface plate + feeler gauge or long straight edge, 2 directions 平台塞尺, 两个方向 |  |  |
| A7 | Cut squareness & burr 切口垂直度·毛刺 | Squareness ≤ 1 mm ★ / burrs and chips fully removed, edges chamfered 垂直度 ≤ 1 mm ★ / 去毛刺·倒角 | Square + visual and touch check 角尺·目视 |  |  |

One-piece verification — cost-efficient method (proposal): ① full-length UT scan on all pieces ② X-ray photos on 1~2 sample pieces per lot, plus any location indicated by UT ③ attach the films / digital photos to the lot inspection report. 整体性确认(经济方案): ① 全数全长超声波扫查 ② 每批抽1~2支拍X光照片, 超声波有显示的部位加拍 ③ 照片附于该批检验报告。

# B. Surface 外观

| # | Inspection item 检验项目 | Criteria 标准 | Method & points 方法·位置 | Record 记录 | P/F 判定 |
| --- | --- | --- | --- | --- | --- |
| B1 | Dents / impact marks 碰伤·压痕 | Depth ≤ 0.2 mm ★; end zones (100 mm) free of defects 深度 ≤ 0.2 mm ★, 端部100mm内无缺陷 | Full-surface visual + depth gauge on suspect spots 全表面目视+深度尺 |  |  |
| B2 | Scratches 划伤 | Depth ≤ 0.2 mm ★ (within machining allowance) 深度 ≤ 0.2 mm ★ | Full-surface visual under angled light 斜光目视 |  |  |
| B3 | Corrosion / water stain 腐蚀·水渍 | None — pieces with white rust or stains to be set aside for review 不允许 — 发现白锈·水渍的管请单独放置以便确认 | Full-surface visual — please mind sea-freight condensation 目视, 注意海运冷凝 |  |  |
| B4 | Inner surface 内表面 | No coarse defects, embedded foreign matter, or heavy die lines 无粗大缺陷·夹杂·严重模痕 | Flashlight check from both ends 手电筒目视 |  |  |
| B5 | General finish 表面 | Ra 6.3~12.5 level is sufficient (parts will be re-machined); no cracks, blisters, or laps Ra 6.3~12.5即可(后续再加工), 无裂纹·气泡·折叠 | Visual; penetrant test if in doubt 目视, 必要时渗透探伤 |  |  |

# C. Material & Documents 材质·文件

| # | Inspection item 检验项目 | Criteria 标准 | Method & points 方法·位置 | Record 记录 | P/F 判定 |
| --- | --- | --- | --- | --- | --- |
| C1 | MTC cross-check 质保书核对 | EN 10204 3.1, signed and stamped, matching our lot and size, product standard stated EN 10204 3.1, 签字盖章, 与订单批号·规格一致, 注明产品标准 | Check labels / markings against MTC lot numbers, all pieces 标签与质保书批号核对 |  |  |
| C2 | Alloy & temper check 牌号·状态 | 6061-T6 — hardness ≥ 95 HBW / conductivity 40~47 %IACS ★ 6061-T6 — 硬度 ≥95 HBW / 电导率 40~47 %IACS ★ | Portable hardness tester + eddy-current conductivity meter, at least 1 point per piece 硬度计+电导率仪, 每支至少1点 |  |  |
| C3 | Internal soundness report 内部质量报告 | X-ray or UT report attached per lot (as requested) 每批附X光或超声波报告 | Confirm report received and test locations marked 核对报告及测试部位 |  |  |
| C4 | Billet origin 铸锭来源 | Billet source and composition (Fe etc.) stated in MTC; if recycled billet is used, please state it 质保书注明铸锭来源·成分; 如使用再生铸锭请注明 | Check MTC entries 核对质保书 |  |  |

# D. Packing & Transport 包装·运输 — important for 3 m long tubes 长管必备

| # | Inspection item 检验项目 | Criteria 标准 | Method & points 方法·位置 | Record 记录 | P/F 判定 |
| --- | --- | --- | --- | --- | --- |
| D1 | Multi-point support 多点支撑 | 3 m tubes: at least 3 supports to prevent permanent bow from sagging 3m长管至少3点支撑, 防止下垂弯曲 | Check support positions in crate; pre-shipment photos appreciated 装箱支撑确认, 请提供装箱照片 |  |  |
| D2 | End protection 管口保护 | Caps / covers on both ends — protect cut faces from impact and foreign matter 两端加保护帽, 防磕碰·防异物 | Visual, all pieces 目视全数 |  |  |
| D3 | Padding & separation 缓冲·隔离 | No metal-to-metal contact between tubes; protective pads under strapping 管间不得金属接触, 打包带处加保护垫 | Check at unpacking 开箱确认 |  |  |
| D4 | Moisture barrier 防潮 | VCI or PE wrap + desiccant — for sea-freight condensation VCI或PE+干燥剂, 防海运冷凝 | Check wrap and desiccant 防潮包装确认 |  |  |
| D5 | Handling 装卸 | Fabric slings only (no bare wire rope); no single-point lifting 请用吊装带(不用钢丝绳直接吊), 不得单点起吊 | Witness loading / unloading 监装监卸 |  |  |

# E. Measurement Record per Piece 实测记录

Piece No. 管号: ________    Size 规格: ________________

| Position 位置 | OD 0° | OD 90° | t 0° | t 90° | t 180° | t 270° |
| --- | --- | --- | --- | --- | --- | --- |
| End A (50mm) |  |  |  |  |  |  |
| Middle 中间 |  |  |  |  |  |  |
| End B (50mm) |  |  |  |  |  |  |

Roundness 圆度:  End A ______ mm  /  Middle ______ mm  /  End B ______ mm      Straightness 直线度: ______ mm / full length

Hardness 硬度: ______ HBW      Conductivity 电导率: ______ %IACS      Result 判定: Pass 合格 ☐  /  Review needed 需确认 ☐

Inspector 检验员: ____________      Supplier confirmation 供方确认: ____________

If any item falls outside the criteria: please set the affected piece aside, share photos with us, and we will review together and agree on the solution (rework, replacement, etc.) before shipment. 如有超出标准的项目: 请将该支单独放置并拍照告知, 双方共同确认后商定处理方案(修复·更换等)再安排出货。